Chapter 3: Research Methodology

3.1 Introduction

This chapter presents the comprehensive methodology adopted to investigate the structural reliability of timber roof trusses under fire exposure. The research methodology integrates experimental characterization of material properties, fire performance testing, and probabilistic reliability analysis using Monte Carlo Simulation. The chapter is structured to provide a detailed account of the experimental procedures, analytical models, and computational frameworks employed to achieve the research objectives outlined in Section 1.4.

The methodology focuses specifically on the identification, formulation, and probabilistic assessment of critical failure modes in timber truss members—namely the top chord, bottom chord, and web members—under standard and parametric fire exposures. Connections are excluded from this investigation as per the scope defined in Section 1.5.1.

3.2 Research Design

This study employs a sequential mixed-methods approach comprising three interconnected phases:

Phase 1: Material Characterization

- Determination of physical properties (density, moisture content)

- Evaluation of mechanical properties (modulus of elasticity, modulus of rupture, compressive strength, tensile strength, shear strength)

- Strength classification according to EN 338

- Statistical distribution fitting for probabilistic modeling

Phase 2: Fire Performance Assessment

- Experimental determination of charring rates under standard (ISO 834) and parametric fire exposures

- Evaluation of fire-retardant treatment efficacy

- Development of time-dependent degradation models

Phase 3: Probabilistic Reliability Analysis

- Formulation of limit state functions for each failure mode

- Monte Carlo Simulation incorporating material and fire scenario variability

- Sensitivity analysis to identify critical parameters

- Validation against experimental observations

3.3 Identification of Failure Modes in Timber Trusses

3.3.1 Classification of Failure Modes

Based on an extensive literature review and preliminary structural analysis, the failure modes investigated in this study are classified into three categories corresponding to the principal truss members:

Table 3.1: Classification of Failure Modes by Member Type

| Member Type | Failure Mode | Failure Mechanism |
| --- | --- | --- |
| Top Chord | Compression Buckling | Loss of stability under axial compression due to slenderness |
|  | Combined Bending and Compression | Interaction between axial force and bending moment |
|  | Shear | Transverse failure parallel to grain at support regions |
|  | Bending | Flexural failure between nodes |
| Bottom Chord | Tension Rupture | Tensile fracture parallel to grain |
|  | Bending | Flexural failure due to self-weight and eccentricity |
|  | Lateral Torsional Buckling | Instability of compression flange in bending |
|  | Shear | Transverse failure at connections |
| Web Members | Compression Buckling | Stability failure in diagonal and vertical compression members |
|  | Tension Rupture | Tensile failure in diagonal tension members |
|  | Shear | Transverse failure at member ends |

3.3.2 Theoretical Basis for Failure Mode Formulation

The limit state design philosophy adopted in Eurocode 5 forms the theoretical foundation for failure mode formulation. For each failure mode, a limit state function is established in the general form:

Eqn. 3.1: Gi(X)=Ri(X)-Si(X)

where:

- Gi(X) = performance function for failure mode i

- Ri(X) = structural resistance for failure mode i

- Si(X) = load effect for failure mode i

- X = vector of random variables

Failure occurs when: Gi(X)≤0
Safe state when: Gi(X)>0

The probability of failure for each mode is:

Eqn. 3.2: Pf,i=P[Gi(X)≤0]

3.4 Failure Mode 1: Top Chord Compression Buckling

3.4.1 Description of Failure Mechanism

The top chord of a timber truss is subjected to compressive forces from roof loads. Under fire exposure, charring reduces the cross-sectional area, increasing the slenderness ratio and reducing the buckling resistance. Compression buckling occurs when the critical buckling load is exceeded, leading to sudden lateral deflection and structural collapse.

3.4.2 Limit State Formulation

Eqn. 3.3: G1(X)=Rc,buckle-NEd,fi

Resistance Component:

Eqn. 3.4: Rc,buckle=kc,y⋅fc,0,d,fi⋅Aef

Load Effect Component:

Eqn. 3.5: NEd,fi=qfi⋅Lspan28⋅htruss⋅cos⁡α+Nself

3.4.3 Variable Definitions

Buckling Reduction Factor:

Eqn. 3.6: kc,y=1ky+ky2-λrel,y2

Eqn. 3.7: ky=0.51+βc(λrel,y-0.3)+λrel,y2

Relative Slenderness:

Eqn. 3.8: λrel,y=λyπfc,0,kE0,05

Slenderness Ratio:

Eqn. 3.9: λy=Lc,yief,y

Radius of Gyration:

Eqn. 3.10: ief,y=Ief,yAef=hef12

Effective Cross-Sectional Area (3-sided exposure):

Eqn. 3.11: Aef=(b-2def)(h-def)

Effective Char Depth:

Eqn. 3.12: def=β⋅t+7

where:

- fc,0,d,fi = design compressive strength parallel to grain under fire (N/mm²)

- βc=0.2 = imperfection factor for solid timber

- Lc,y = buckling length about y-axis (mm)

- qfi = fire load intensity (kN/m)

- Lspan = total truss span (m)

- htruss = truss height at apex (m)

- α = roof pitch angle (degrees)

- β = charring rate (mm/min)

- t = fire exposure time (min)

- b,h = initial member width and depth (mm)

3.4.4 Random Variables

Eqn. 3.13: X1={fc,0,k,E0,05,ρ,β,MC,b,h,L,qfi,t}

3.5 Failure Mode 2: Top Chord Combined Bending and Compression

3.5.1 Description of Failure Mechanism

The top chord experiences both axial compression and bending moments due to:

- Eccentricity between nodes

- Continuous beam action over multiple supports

- Fire-induced neutral axis shift due to non-uniform charring

The interaction between these stress components can lead to failure even when individual checks are satisfied.

3.5.2 Limit State Formulation (EN 1995-1-1, Equation 6.23)

Eqn. 3.14: G2(X)=1.0-σc,0,dkc,y⋅fc,0,d,fi2σm,y,dfm,d,fi

3.5.3 Variable Definitions

Compressive Stress:

Eqn. 3.15: σc,0,d=NEd,fiAef

Bending Stress:

Eqn. 3.16: σm,y,d=MEd,fiWef,y

Bending Moment:

Eqn. 3.17: MEd,fi=Mcontinuous+NEd,fi⋅efire

Fire-Induced Eccentricity:

Eqn. 3.18: efire=hef2-h-def2

Section Modulus:

Eqn. 3.19: Wef,y=bef⋅hef26

Design Bending Strength Under Fire:

Eqn. 3.20: fm,d,fi=kfi⋅fm,kγM,fi

where:

- NEd,fi = design axial force under fire (N)

- Mcontinuous = moment from continuous beam action (Nmm)

- kfi=1.0 = modification factor for fire (unprotected)

- γM,fi=1.0 = partial safety factor for fire

3.5.4 Random Variables

Eqn. 3.21: X2={fc,0,k,fm,k,E0,05,β,MC,b,h,L,qfi,efire,t}

3.6 Failure Mode 3: Bottom Chord Tension Rupture

3.6.1 Description of Failure Mechanism

The bottom chord is primarily subjected to tensile forces. Under fire exposure, cross-section reduction increases tensile stress. Failure occurs when the tensile stress exceeds the reduced tensile strength of the heated timber. This is typically a brittle failure mode with limited warning.

3.6.2 Limit State Formulation

Eqn. 3.22: G3(X)=ft,0,d,fi⋅Aef-NEd,fi

3.6.3 Variable Definitions

Design Tension Strength Under Fire:

Eqn. 3.23: ft,0,d,fi=kfi⋅ft,0,kγM,fi

Effective Area (including fastener holes):

Eqn. 3.24: Aef,net=(b-2def-n⋅dhole)⋅(h-def)

Hole Diameter:

Eqn. 3.25: dhole=dfastener+1.0 mm

Tensile Force from Truss Analysis:

Eqn. 3.26: NEd,fi=qfi⋅Lspan28⋅htruss (simplified)

where:

- ft,0,k = characteristic tensile strength parallel to grain (N/mm²)

- n = number of fastener holes in the critical section

- dfastener = fastener diameter (mm)

3.6.4 Random Variables

Eqn. 3.27: X3={ft,0,k,β,MC,b,h,n,dfastener,qfi,t}

3.7 Failure Mode 4: Bottom Chord Bending

3.7.1 Description of Failure Mechanism

Although primarily in tension, the bottom chord experiences bending moments due to:

- Self-weight between nodes

- Eccentricity at connections

- Non-uniform heating causing differential thermal expansion

3.7.2 Limit State Formulation

Eqn. 3.28: G4(X)=fm,d,fi⋅Wef,y-MEd,fi

3.7.3 Variable Definitions

Bending Moment:

Eqn. 3.29: MEd,fi=wself⋅L28+NEd,fi⋅econstruction

Self-Weight:

Eqn. 3.30: wself=ρ⋅g⋅Aef×10-9 kN/mm

Construction Eccentricity:

Eqn. 3.31: econstruction∼Normal(μ=0,σ=5) mm

where:

- g=9.81 m/s2 = gravitational acceleration

- ρ = timber density (kg/m³)

- econstruction = accidental eccentricity from construction tolerances (mm)

3.7.4 Combined Tension and Bending

For sections subjected to both tension and bending, the interaction must be checked:

Eqn. 3.32: G4a(X)=1.0-σt,0,dft,0,d,fiσm,y,dfm,d,fi

3.7.5 Random Variables

Eqn. 3.33: X4={fm,k,ft,0,k,β,MC,ρ,b,h,L,econstruction,qfi,t}

3.8 Failure Mode 5: Bottom Chord Lateral Torsional Buckling

3.8.1 Description of Failure Mechanism

When the bottom chord is subjected to bending, the compression zone (top portion of the chord) can buckle laterally, causing the member to twist and deflect out of plane. This instability failure is particularly critical in fire as the reduced section increases slenderness.

3.8.2 Limit State Formulation (EN 1995-1-1, §6.3.3)

Eqn. 3.34: G5(X)=kcrit⋅fm,d,fi⋅Wef,y-MEd,fi

3.8.3 Variable Definitions

Critical Bending Stress:

Eqn. 3.35: σm,crit=0.78⋅bef2⋅E0,05hef⋅Lef

Relative Slenderness for Bending:

Eqn. 3.36: λrel,m=fm,kσm,crit

Lateral Torsional Buckling Factor:

Eqn. 3.37: kcrit=1.0for λrel,m≤0.751.56-0.75λrel,mfor 0.75<λrel,m≤1.41λrel,m2for λrel,m>1.4

Effective Length for LTB:

Eqn. 3.38: Lef=L⋅kltb

where:

- kltb = factor depending on support conditions and load distribution

- L = member length between lateral restraints (mm)

3.8.4 Random Variables

Eqn. 3.39: X5={fm,k,E0,05,β,b,h,L,Lef,qfi,t}

3.9 Failure Mode 6: Web Member Compression Buckling

3.9.1 Description of Failure Mechanism

Diagonal and vertical web members in compression are among the most slender elements in a truss. Under fire exposure, rapid cross-section reduction increases slenderness, making them susceptible to buckling failure. This can trigger progressive collapse of the entire truss system.

3.9.2 Limit State Formulation

Eqn. 3.40: G6(X)=kc⋅fc,0,d,fi⋅Aef-NEd,fi,web

3.9.3 Variable Definitions

Web Member Forces from Truss Analysis:

For diagonal web members:

Eqn. 3.41: Ndiag=qfi⋅Lpanel2sin⁡θweb

For vertical web members:

Eqn. 3.42: Nvert=qfi⋅Lpanel

Buckling in Both Axes:

Due to the slenderness of web members, buckling must be checked about both principal axes:

Eqn. 3.43: kc=min⁡(kc,y,kc,z)

Effective Length Factors:

Eqn. 3.44: Leff,y=kend,y⋅L

Eqn. 3.45: Leff,z=kend,z⋅L

Eqn. 3.46: kend∼Uniform(0.7,1.0)

where:

- Lpanel = panel length along the chord (mm)

- θweb = angle of diagonal web relative to horizontal (degrees)

- kend = end condition factor (0.7 for fixed ends, 1.0 for pinned ends)

3.9.4 Random Variables

Eqn. 3.47: X6={fc,0,k,E0,05,β,MC,b,h,L,kend,y,kend,z,qfi,t}

3.10 Failure Mode 7: Web Member Tension Rupture

3.10.1 Description of Failure Mechanism

Some diagonal web members are subjected to tensile forces. Similar to the bottom chord, failure occurs when the tensile stress exceeds the reduced tensile strength of the heated timber.

3.10.2 Limit State Formulation

Eqn. 3.48: G7(X)=ft,0,d,fi⋅Aef-NEd,fi,web

3.10.3 Variable Definitions

Tensile Force in Diagonal Web:

Eqn. 3.49: Nt,diag=qfi⋅Lpanel2sin⁡θweb (for tension diagonals)

Effective Area (including possible fastener holes):

Eqn. 3.50: Aef,net=(b-2def-n⋅dhole)⋅(h-def)

3.10.4 Random Variables

Eqn. 3.51: X7={ft,0,k,β,MC,b,h,n,dhole,qfi,t}

3.11 Failure Mode 8: Shear Failure

3.11.1 Description of Failure Mechanism

Shear failure is particularly critical in timber structures under fire because:

- Shear stresses are highest near supports where charring is often most severe

- Timber has relatively low shear strength parallel to grain

- Shear failure is brittle and can occur suddenly without warning

All truss members (top chord, bottom chord, and web members) are susceptible to shear failure at their ends.

3.11.2 Limit State Formulation

Eqn. 3.52: G8(X)=fv,d,fi⋅Aef,shear-VEd,fi

3.11.3 Variable Definitions

Shear Force Distribution:

Maximum shear occurs at supports:

Eqn. 3.53: VEd,fi,max=qfi⋅Lspan2

This shear is distributed among members meeting at the support node:

Eqn. 3.54: VEd,fi,member=VEd,fi,maxnmembers⋅kdist

Shear Stress in Rectangular Section:

Eqn. 3.55: τd=1.5⋅VEd,fi,memberAef,shear

Effective Area for Shear:

Eqn. 3.56: Aef,shear=23⋅bef⋅hef (for rectangular sections, shear area ≈ 2/3 of gross area)

Design Shear Strength Under Fire:

Eqn. 3.57: fv,d,fi=kfi⋅fv,kγM,fi

where:

- nmembers = number of members sharing shear at the support

- kdist = shear distribution factor (depends on member stiffness)

- fv,k = characteristic shear strength (N/mm²)

3.11.4 Shear Verification for Each Member

Top Chord at Support:

Eqn. 3.58: τd,top=1.5⋅Vtopb-2def)⋅(h-def

Bottom Chord at Support:

Eqn. 3.59: τd,bottom=1.5⋅Vbottomb-2def)⋅(h-def

Web Members at Support:

Eqn. 3.60: τd,web=1.5⋅Vwebb-2def)⋅(h-def

3.11.5 Random Variables

Eqn. 3.61: X8={fv,k,β,MC,b,h,qfi,nmembers,kdist,t}

3.12 Summary of Limit State Functions

Table 3.2: Summary of Limit State Functions for All Failure Modes

| Failure Mode | Member | Limit State Function | Equation |
| --- | --- | --- | --- |
| FM1 | Top Chord | G1=kc,y⋅fc,0,d,fi⋅Aef-NEd,fi | Eqn. 3.3 |
| FM2 | Top Chord | G2=1.0-σc,0,dkc,yfc,0,d,fi2σm,y,dfm,d,fi | Eqn. 3.14 |
| FM3 | Bottom Chord | G3=ft,0,d,fi⋅Aef-NEd,fi | Eqn. 3.22 |
| FM4 | Bottom Chord | G4=fm,d,fi⋅Wef,y-MEd,fi | Eqn. 3.28 |
| FM4a | Bottom Chord | G4a=1.0-σt,0,dft,0,d,fiσm,y,dfm,d,fi | Eqn. 3.32 |
| FM5 | Bottom Chord | G5=kcrit⋅fm,d,fi⋅Wef,y-MEd,fi | Eqn. 3.34 |
| FM6 | Web (Comp.) | G6=kc⋅fc,0,d,fi⋅Aef-NEd,fi,web | Eqn. 3.40 |
| FM7 | Web (Tension) | G7=ft,0,d,fi⋅Aef-NEd,fi,web | Eqn. 3.48 |
| FM8 | All Members | G8=fv,d,fi⋅Aef,shear-VEd,fi,member | Eqn. 3.52 |

3.13 Time-Dependent Degradation Modeling

3.13.1 Char Depth Progression

Eqn. 3.62: dchar(t)=β⋅t for 0≤t≤tfire

Eqn. 3.63: def(t)=β⋅t+7 (effective char depth including zero-strength layer)

3.13.2 Temperature Distribution in Cross-Section

Eqn. 3.64: T(x,t)=T0+[Tfire(t)-T0]⋅exp⁡xα⋅t

where:

- x = depth from char front (mm)

- α = thermal diffusivity (mm²/min)

- T0 = ambient temperature (20°C)

- Tfire(t) = fire compartment temperature at time t (°C)

3.13.3 Temperature-Dependent Strength Reduction (EN 1995-1-2)

Eqn. 3.65: kmod,fi(T)=1.0T≤20∘C1-0.005(T-20)20∘C<T≤300∘C0T>300∘C

3.13.4 Time-Dependent Resistance

Eqn. 3.66: Ri(t)=Ri(0)⋅kmod,fi(T)⋅Aef(t)A0⋅Wef(t)W0

3.14 Experimental Determination of Input Parameters

3.14.1 Material Properties Testing

The mechanical properties required for each failure mode are determined experimentally following EN 408 and EN 384:

Table 3.3: Material Properties and Test Methods

| Property | Symbol | Test Method | Specimens |
| --- | --- | --- | --- |
| Bending strength | fm,k | 4-point bending (EN 408) | 40 per species |
| Modulus of elasticity | E0,mean | 3-point bending (EN 408) | 40 per species |
| Compression strength | fc,0,k | Compression parallel to grain | 30 per species |
| Tension strength | ft,0,k | Tension parallel to grain | 30 per species |
| Shear strength | fv,k | Block shear test | 30 per species |
| Density | ρ | Oven-dry method (EN 13183-1) | 40 per species |
| Moisture content | MC | Oven-dry method (EN 13183-1) | 40 per species |

3.14.2 Charring Rate Determination

Charring rates are determined from furnace tests under three fire scenarios:

Eqn. 3.67: β=dchar,avgtexposure

Table 3.4: Fire Test Scenarios for Charring Rate Determination

| Fire Test | Scenario | Opening Factor | Duration | Specimens |
| --- | --- | --- | --- | --- |
| FTI | Standard (ISO 834) | N/A | 60 min | 20 per species |
| FTII | Kitchen (low ventilation) | 0.028 m⁰·⁵ | 62.4 min | 20 per species |
| FTIII | Sitting room (high ventilation) | 0.137 m⁰·⁵ | 23.6 min | 20 per species |

3.15 Probabilistic Framework for Failure Mode Analysis

3.15.1 Random Variable Distributions

Based on experimental characterization, the following distributions are assigned:

Eqn. 3.68: fm,k∼Lognormal(μfm,σfm)

Eqn. 3.69: fc,0,k∼Lognormal(μfc,σfc)

Eqn. 3.70: ft,0,k∼Lognormal(μft,σft)

Eqn. 3.71: fv,k∼Lognormal(μfv,σfv)

Eqn. 3.72: E0,05∼Lognormal(μE,σE)

Eqn. 3.73: ρ∼Normal(μρ,σρ)

Eqn. 3.74: MC∼Normal(μMC,σMC)

Eqn. 3.75: β∼Lognormal(μβ,σβ)

Eqn. 3.76: qfi∼Gumbel(μq,σq)

Eqn. 3.77: b,h,L∼Normal(μ,σ)

3.15.2 Correlation Structure (Based on JCSS Probabilistic Model Code)

Eqn. 3.78: Corr(fm,k,fc,0,k)=0.8

Eqn. 3.79: Corr(fm,k,E0,05)=0.7

Eqn. 3.80: Corr(fc,0,k,ρ)=0.6

Eqn. 3.81: Corr(β,ρ)=-0.5 (denser wood chars slower)

Eqn. 3.82: Corr(β,MC)=0.3 (wetter wood chars slower initially)

3.15.3 Monte Carlo Simulation Algorithm for Multiple Failure Modes

Step 1: Initialize

- Nsim=106 (number of simulations)

- failures[k]=0 for k=1 to 8 (failure counters)

- t=0 to 120 min (time steps)

Step 2: For each simulation i=1 to Nsim:

- Sample random variables Xi from distributions in Eqs. 3.68-3.77

- Apply correlation structure (Eqs. 3.78-3.82)

- For each time step tj:

  - Calculate def(tj)=βi⋅tj+7

  - Update Aef(tj), Wef(tj), ief(tj) for each member

  - Calculate temperature T(tj) from fire curve

  - Determine kmod,fi(T) from Eqn. 3.65

  - For each failure mode k=1 to 8:

    - Calculate Rk(tj) using appropriate equations (Table 3.2)

    - Calculate Sk(tj) from load effects

    - Evaluate Gk(Xi,tj)

    - If Gk≤0:

      - Increment failures[k]

      - Record time to failure tfail,k=tj

      - Break time loop for this mode

Step 3: Compute probabilities:

Eqn. 3.83: Pf,k=failures[k]Nsim,k=1,…,8

Step 4: System probability of failure (series system):

Eqn. 3.84: Pf,system=1-k=18(1-Pf,k)

Step 5: Reliability indices:

Eqn. 3.85: βk=-Φ-1(Pf,k)

Eqn. 3.86: βsystem=-Φ-1(Pf,system)

3.16 Sensitivity Analysis

To identify the most critical parameters influencing each failure mode, Sobol' sensitivity indices are calculated:

Eqn. 3.87: STi=Var[E(Gk∣X∼i)]Var(Gk)

where:

- STi = total sensitivity index for variable i

- X∼i = vector of all variables except i

- Var(Gk) = total variance of the limit state function

Variables with highest STi are identified as critical for each failure mode.

3.17 Validation Framework

3.17.1 Validation Against Experimental Charring Rates

Eqn. 3.88: εchar=∣βMCS-βexp∣βexp×100%≤10%

3.17.2 Validation of Failure Probabilities

Eqn. 3.89: εPf=∣Pf,MCS-Pf,exp∣Pf,exp×100%≤15%

where Pf,exp is estimated from small-scale fire tests.

3.17.3 Convergence Criteria

Eqn. 3.90: ∣Pf(N)-Pf(N/2)Pf(N/2)∣≤0.05 for N≥106

3.18 Summary

This chapter has presented a comprehensive methodology for investigating eight distinct failure modes in timber roof trusses under fire exposure:

- Top Chord Compression Buckling (FM1)

- Top Chord Combined Bending and Compression (FM2)

- Bottom Chord Tension Rupture (FM3)

- Bottom Chord Bending (FM4)

- Bottom Chord Lateral Torsional Buckling (FM5)

- Web Member Compression Buckling (FM6)

- Web Member Tension Rupture (FM7)

- Shear Failure in All Members (FM8)

For each failure mode, explicit limit state functions have been formulated (Eqns. 3.3-3.61), random variables defined (Eqns. 3.68-3.77), and correlation structures established (Eqns. 3.78-3.82). The Monte Carlo simulation framework (Section 3.15.3) enables probabilistic assessment of failure probabilities and reliability indices for each mode, while sensitivity analysis (Section 3.16) identifies the most critical parameters governing truss performance under fire.

The methodology integrates experimental data from material characterization and fire tests with advanced probabilistic modeling, providing a robust framework for evaluating the fire reliability of Nigerian timber species (Anogeissus leiocarpa and Erythrophleum suaveolens) in roof truss applications.

Chapter 4: EC5 Deterministic design

4.1 Introduction

This chapter presents the results of the deterministic Eurocode 5 fire design calculations for a timber roof truss with a span of 6 m. The analysis follows the methodology established in Chapter 3 and utilizes the experimentally determined material properties for Erythrophleum suaveolens (R) and Anogeissus leiocarpa (W) from Section 4.1. The calculations verify the structural performance of all truss members—top chord, bottom chord, and web members—under standard fire exposure for a required fire resistance of R30 (30 minutes). Connections are excluded from this analysis as per the scope defined in Section 1.5.1.

4.2 Design Basis and Assumptions

Standard: EN 1995-1-2:2004 (Eurocode 5: Design of timber structures – Part 1-2: Structural fire design)

Fire Exposure: Standard fire curve (ISO 834) according to EN 1363-1

Fire Resistance Requirement: R30 (30 minutes load-bearing capacity)

Truss Configuration: Double-Howe truss, span L = 6 m, height h = L/6 = 1.0 m

Reference: Experimental data for Erythrophleum suaveolens (R) and Anogeissus leiocarpa (W) from Section 4.1

4.3 Input Parameters

4.3.1 Material Properties (from experimental data)

Table 4.1: Experimentally Determined Bending Strength and MOE

| Species | Bending Strength fm,k (N/mm²) | Mean MOE E0,mean (N/mm²) | Source |
| --- | --- | --- | --- |
| E. suaveolens (R) | 38.9 | 8935 | Table 4.5 |
| A. leiocarpa (W) | 22.7 | 4612 | Table 4.5 |

4.3.2 Derived Reference Properties from Experimental Data

Based on the experimentally determined bending strength values, the complete sets of characteristic material properties for both species were derived using established correlations from EN 338 and the JCSS Probabilistic Model Code.

Table 4.2: Derived Reference Properties for Anogeissus leiocarpa (W)

| Property | Symbol | Formula | Value |
| --- | --- | --- | --- |
| Bending strength | fm,k | Experimental | 22.7 N/mm² |
| Tension parallel | ft,0,k | 0.6 fm,k | 13.6 N/mm² |
| Compression parallel | fc,0,k | 0.45 fm,k | 10.2 N/mm² |
| Shear | fv,k | 0.067 fm,k | 1.52 N/mm² |
| Tension perpendicular | ft,90,k | 0.015 fm,k | 0.34 N/mm² |
| Compression perpendicular | fc,90,k | 0.20 fc,0,k | 2.04 N/mm² |
| Mean MOE | E0,mean | Experimental | 4612 N/mm² |
| 5th percentile MOE | E0,05 | 0.67 E0,mean | 3090 N/mm² |
| MOE perpendicular | E90,mean | E0,mean / 30 | 154 N/mm² |
| Shear modulus | Gmean | E0,mean / 16 | 288 N/mm² |

Table 4.3: Derived Reference Properties for Erythrophleum suaveolens (R)

| Property | Symbol | Formula | Value |
| --- | --- | --- | --- |
| Bending strength | fm,k | Experimental | 38.9 N/mm² |
| Tension parallel | ft,0,k | 0.6 fm,k | 23.3 N/mm² |
| Compression parallel | fc,0,k | 0.45 fm,k | 17.5 N/mm² |
| Shear | fv,k | 0.067 fm,k | 2.61 N/mm² |
| Tension perpendicular | ft,90,k | 0.015 fm,k | 0.58 N/mm² |
| Compression perpendicular | fc,90,k | 0.20 fc,0,k | 3.50 N/mm² |
| Mean MOE | E0,mean | Experimental | 8935 N/mm² |
| 5th percentile MOE | E0,05 | 0.67 E0,mean | 5986 N/mm² |
| MOE perpendicular | E90,mean | E0,mean / 30 | 298 N/mm² |
| Shear modulus | Gmean | E0,mean / 16 | 558 N/mm² |

4.3.3 Charring Rates (from experimental data – Section 4.2)

Table 4.4: Charring Rates for Selected Timber Species

| Species | Condition | Charring Rate βn (mm/min) | Source |
| --- | --- | --- | --- |
| E. suaveolens (R) | Untreated | 0.65 | Table 4.6 |
| E. suaveolens (R) | Treated | 0.57 | Table 4.6 |
| A. leiocarpa (W) | Untreated | 0.71 | Table 4.6 |
| A. leiocarpa (W) | Treated | 0.57 | Table 4.6 |

Selected for baseline calculation: Untreated E. suaveolens with βn=0.65 mm/min

4.3.4 Geometric Properties

Table 4.5: Initial Member Dimensions

| Member | Symbol | Top Chord | Bottom Chord | Web (Diagonal) | Web (Vertical) |
| --- | --- | --- | --- | --- | --- |
| Width | b | 75 mm | 75 mm | 50 mm | 50 mm |
| Depth | h | 150 mm | 150 mm | 100 mm | 100 mm |
| Length | L | 1500 mm | 1500 mm | 1800 mm | 1000 mm |
| Exposure | - | 3 sides | 3 sides | 3 sides | 3 sides |

4.3.5 Loading (Fire Situation – Accidental Combination per EN 1990)

Eqn. 4.1: qfi=Gk+ψ2Qk

Table 4.6: Load Parameters

| Parameter | Symbol | Value |
| --- | --- | --- |
| Permanent load | Gk | 2.5 kN/m |
| Variable load (snow) | Qk | 1.8 kN/m |
| Combination factor | ψ2 | 0.2 (snow load) |
| Design fire load | qfi | 2.5 + 0.2 × 1.8 = 2.86 kN/m |

4.3.6 Partial Safety Factors for Fire (EN 1995-1-2, §2.3)

Table 4.7: Partial Safety Factors

| Factor | Symbol | Value |
| --- | --- | --- |
| Material factor for fire | γM,fi | 1.0 |
| Modification factor for fire | kfi | 1.0 (unprotected) |

4.4 Charring Calculations (EN 1995-1-2, §3.4)

4.4.1 General Charring Formulation

Eqn. 4.2: dchar,n=βn⋅t (char depth)

Eqn. 4.3: def=dchar,n+k0⋅d0 (effective char depth)

where:

- βn = notional charring rate (mm/min)

- t = fire exposure time (min)

- d0=7 mm (zero-strength layer)

- k0=1.0 for t≥20 minutes

4.4.2 Char Depth After 30 Minutes

For untreated E. suaveolens (βn=0.65 mm/min):

Eqn. 4.4: dchar,n=0.65×30=19.5 mm

Eqn. 4.5: def=19.5+1.0×7=26.5 mm

4.4.3 Effective Cross-Section Dimensions by Member Type

4.4.3.1 Top Chord (3-sided exposure)

Eqn. 4.6: bef=b-2⋅def=75-2×26.5=22.0 mm

Eqn. 4.7: hef=h-def=150-26.5=123.5 mm

4.4.3.2 Bottom Chord (3-sided exposure)

Eqn. 4.8: bef=b-2⋅def=75-2×26.5=22.0 mm

Eqn. 4.9: hef=h-def=150-26.5=123.5 mm

4.4.3.3 Web Members (3-sided exposure)

For diagonal web with initial dimensions 50 mm × 100 mm:

Eqn. 4.10: bef=50-2×26.5=-3.0 mm → Not acceptable!

Observation: The web member would be completely charred through at 30 minutes. For R30, web members require larger initial dimensions or fire protection.

Revised web dimensions for R30: Increase to b=75 mm, h=100 mm

Eqn. 4.11: bef=75-2×26.5=22.0 mm

Eqn. 4.12: hef=100-26.5=73.5 mm

4.4.4 Summary of Effective Cross-Sections (t = 30 min)

Table 4.8: Effective Cross-Sectional Properties at 30 Minutes

| Member | Initial b×h (mm) | Effective bef×hef (mm) | Aef (mm²) |
| --- | --- | --- | --- |
| Top Chord | 75 × 150 | 22.0 × 123.5 | 2,717 |
| Bottom Chord | 75 × 150 | 22.0 × 123.5 | 2,717 |
| Diagonal Web | 75 × 100 | 22.0 × 73.5 | 1,617 |
| Vertical Web | 75 × 100 | 22.0 × 73.5 | 1,617 |

4.5 Section Properties After Charring

4.5.1 General Formulations

Eqn. 4.13: Aef=bef⋅hef (area)

Eqn. 4.14: Ief,y=bef⋅hef312 (moment of inertia about y-axis)

Eqn. 4.15: Ief,z=hef⋅bef312 (moment of inertia about z-axis)

Eqn. 4.16: ief,y=Ief,yAef (radius of gyration about y-axis)

Eqn. 4.17: ief,z=Ief,zAef (radius of gyration about z-axis)

Eqn. 4.18: Wef,y=bef⋅hef26 (section modulus about y-axis)

Eqn. 4.19: Wef,z=hef⋅bef26 (section modulus about z-axis)

4.5.2 Calculated Section Properties at t = 30 min

Table 4.9: Section Properties After 30 Minutes of Fire Exposure

| Member | Aef (mm²) | Ief,y (×10⁶ mm⁴) | Wef,y (×10³ mm³) | ief,y (mm) | ief,z (mm) |
| --- | --- | --- | --- | --- | --- |
| Top Chord | 2,717 | 3.44 | 55.8 | 35.6 | 6.35 |
| Bottom Chord | 2,717 | 3.44 | 55.8 | 35.6 | 6.35 |
| Diagonal Web | 1,617 | 0.73 | 19.8 | 21.2 | 6.35 |
| Vertical Web | 1,617 | 0.73 | 19.8 | 21.2 | 6.35 |

4.6 Internal Forces from Truss Analysis

From structural analysis under fire loading (qfi=2.86 kN/m) for a 6 m span truss:

Table 4.10: Member Forces at t = 0 and t = 30 min

| Member | Force Type | Initial Force (kN) | Force at 30 min (kN)¹ | Design Force FEd,fi (kN) |
| --- | --- | --- | --- | --- |
| Top Chord | Compression | -21.3 | -17.8 | -17.8 |
| Bottom Chord | Tension | +19.1 | +16.1 | +16.1 |
| Diagonal Web | Compression | -9.2 | -7.8 | -7.8 |
| Diagonal Web | Tension | +7.6 | +6.4 | +6.4 |
| Vertical Web | Compression | -6.3 | -5.3 | -5.3 |

¹Forces reduced due to stiffness loss in heated members (simplified 15% reduction).

4.7 Design Strength Under Fire

The design strength of timber under fire conditions is determined according to EN 1995-1-2, §2.3. For the accidental fire situation, the partial safety factor for material properties γM,fi is taken as 1.0, and the modification factor for fire kfi is 1.0 for unprotected members. Therefore, the design strength in fire equals the characteristic strength:

Eqn. 4.20: fd,fi=kfi⋅fkγM,fi=1.0⋅fk1.0=fk

4.7.1 Material Strengths for Verification

For the deterministic fire design calculations, the characteristic strengths derived from experimental data in Tables 4.2 and 4.3 are adopted as the design strengths under fire conditions. A summary of the key strength properties for verification of each failure mode is provided in Table 4.11.

Table 4.11: Design Strengths Under Fire

| Strength Type | Symbol | E. suaveolens (R) (N/mm²) | A. leiocarpa (W) (N/mm²) |
| --- | --- | --- | --- |
| Bending | fm,d,fi | 38.9 | 22.7 |
| Compression parallel | fc,0,d,fi | 17.5 | 10.2 |
| Tension parallel | ft,0,d,fi | 23.3 | 13.6 |
| Shear | fv,d,fi | 2.61 | 1.52 |

4.8 FAILURE MODE 1: TOP CHORD – COMPRESSION BUCKLING

4.8.1 Buckling About Strong Axis (y-y) for E. suaveolens (R)

Slenderness Ratio:

Eqn. 4.21: λy=Lief,y=150035.6=42.1

Relative Slenderness:

Eqn. 4.22: λrel,y=λyπfc,0,kE0,05

For E. suaveolens with fc,0,k=17.5 N/mm² and E0,05=5986 N/mm²:

Eqn. 4.23: λrel,y=42.1π17.55986=0.41

Instability Factor:

Eqn. 4.24: ky=0.51+βc(λrel,y-0.3)+λrel,y2

where βc=0.2 for solid timber

Eqn. 4.25: ky=0.51+0.2(0.41-0.3)+0.412=0.5(1+0.022+0.168)=0.595

Eqn. 4.26: kc,y=1ky+ky2-λrel,y2=10.595+0.5952-0.412=0.96

4.8.2 Buckling About Weak Axis (z-z) for E. suaveolens (R)

Slenderness Ratio:

Eqn. 4.27: λz=Lief,z=15006.35=236.2

Relative Slenderness:

Eqn. 4.28: λrel,z=236.2π17.55986=2.35

Since λrel,z>3.0, the member is extremely slender about the z-axis. Lateral restraint is required at intervals to prevent buckling about the weak axis.

Assumption: Lateral restraints provided at 750 mm spacing

Eqn. 4.29: λz=7506.35=118.1

Eqn. 4.30: λrel,z=118.1π17.55986=1.17

Eqn. 4.31: kz=0.51+0.2(1.17-0.3)+1.172=0.5(1+0.174+1.369)=1.272

Eqn. 4.32: kc,z=11.272+1.2722-1.172=0.57

4.8.3 Buckling Verification for E. suaveolens (R)

Compressive Stress:

Eqn. 4.33: σc,0,d=NEd,fiAef=17.8×1032717=6.55 N/mm²

Verification (strong axis buckling):

Eqn. 4.34: σc,0,dkc,y⋅fc,0,d,fi=6.550.96×17.5=6.5516.80=0.39≤1.0 ✓ PASS

Verification (weak axis buckling with restraints):

Eqn. 4.35: σc,0,dkc,z⋅fc,0,d,fi=6.550.57×17.5=6.559.98=0.66≤1.0 ✓ PASS

Conclusion: The top chord satisfies both strong and weak axis buckling requirements with lateral restraints at 750 mm spacing. The utilization ratio of 0.66 for weak-axis buckling indicates adequate performance.

4.8.4 Buckling Verification for A. leiocarpa (W)

For A. leiocarpa with fc,0,k=10.2 N/mm² and E0,05=3090 N/mm²:

Strong axis:

Eqn. 4.36: λrel,y=42.1π10.23090=0.43

Eqn. 4.37: ky=0.5[1+0.2(0.43-0.3)+0.432]=0.5(1+0.026+0.185)=0.606

Eqn. 4.38: kc,y=0.95

Eqn. 4.39: 6.550.95×10.2=6.559.69=0.68≤1.0 ✓ PASS

Weak axis (with restraints at 750 mm):

Eqn. 4.40: λrel,z=118.1π10.23090=1.21

Eqn. 4.41: kz=0.5[1+0.2(1.21-0.3)+1.212]=0.5(1+0.182+1.464)=1.323

Eqn. 4.42: kc,z=0.55

Eqn. 4.43: 6.550.55×10.2=6.555.61=1.17>1.0 ✗ FAIL

Conclusion for A. leiocarpa: The top chord fails in weak-axis buckling with utilization 1.17, requiring either closer lateral restraint spacing or increased member dimensions.

4.9 FAILURE MODE 2: BOTTOM CHORD – TENSION RUPTURE

4.9.1 Tension Verification for E. suaveolens (R)

Eqn. 4.44: σt,0,d=NEd,fiAef=16.1×1032717=5.93 N/mm²

Eqn. 4.45: σt,0,dft,0,d,fi=5.9323.3=0.25≤1.0 ✓ PASS

4.9.2 Tension with Bending (due to self-weight)

Bending moment due to self-weight:

Eqn. 4.46: Mself=γwood⋅Aef⋅L28

where γwood=7.45 kN/m³ (density × gravity)

Eqn. 4.47: Mself=7.45×10-6×2717×150028=5.69 Nm = 0.00569 kNm

Bending stress:

Eqn. 4.48: σm,y,d=MselfWef,y=0.00569×10655.8×103=0.10 N/mm²

Combined tension and bending (EN 1995-1-1, Eq. 6.17):

Eqn. 4.49: σt,0,dft,0,d,fi+σm,y,dfm,d,fi≤1.0

Eqn. 4.50: 5.9323.3+0.1038.9=0.254+0.003=0.257≤1.0 ✓ PASS

4.9.3 Tension Verification for A. leiocarpa (W)

Eqn. 4.51: 5.9313.6=0.44≤1.0 ✓ PASS

Combined tension and bending:

Eqn. 4.52: 5.9313.6+0.1022.7=0.436+0.004=0.44≤1.0 ✓ PASS

Conclusion: Both species satisfy tension requirements with utilization ratios of 0.26 for R and 0.44 for W, indicating adequate capacity.

4.10 FAILURE MODE 3: DIAGONAL WEB – COMPRESSION BUCKLING

4.10.1 Diagonal Web in Compression for E. suaveolens (R)

Member properties:

- Length L=1800 mm

- Effective section: 22.0×73.5 mm

- Aef=1617 mm²

- ief,y=21.2 mm

- ief,z=6.35 mm

- Compression force NEd,fi=-7.8 kN

4.10.2 Buckling About Strong Axis for E. suaveolens (R)

Eqn. 4.53: λy=Lief,y=180021.2=84.9

Eqn. 4.54: λrel,y=84.9π17.55986=0.83

Eqn. 4.55: ky=0.51+0.2(0.83-0.3)+0.832=0.5(1+0.106+0.689)=0.898

Eqn. 4.56: kc,y=10.898+0.8982-0.832=0.79

4.10.3 Buckling About Weak Axis for E. suaveolens (R) (with restraint)

Assumption: Lateral restraint at mid-length (Leff=900 mm)

Eqn. 4.57: λz=9006.35=141.7

Eqn. 4.58: λrel,z=141.7π17.55986=1.41

Eqn. 4.59: kz=0.51+0.2(1.41-0.3)+1.412=0.5(1+0.222+1.988)=1.605

Eqn. 4.60: kc,z=11.605+1.6052-1.412=0.42

4.10.4 Compression Verification for E. suaveolens (R)

Compressive Stress:

Eqn. 4.61: σc,0,d=7.8×1031617=4.82 N/mm²

Strong axis verification:

Eqn. 4.62: 4.820.79×17.5=4.8213.83=0.35≤1.0 ✓ PASS

Weak axis verification (with restraint):

Eqn. 4.63: 4.820.42×17.5=4.827.35=0.66≤1.0 ✓ PASS

4.10.5 Compression Verification for A. leiocarpa (W)

For A. leiocarpa with fc,0,k=10.2 N/mm² and E0,05=3090 N/mm²:

Strong axis:

Eqn. 4.64: λrel,y=84.9π10.23090=0.88

Eqn. 4.65: ky=0.5[1+0.2(0.88-0.3)+0.882]=0.5(1+0.116+0.774)=0.945

Eqn. 4.66: kc,y=0.76

Eqn. 4.67: 4.820.76×10.2=4.827.75=0.62≤1.0 ✓ PASS

Weak axis (with restraint at mid-length):

Eqn. 4.68: λrel,z=141.7π10.23090=1.46

Eqn. 4.69: kz=0.5[1+0.2(1.46-0.3)+1.462]=0.5(1+0.232+2.132)=1.682

Eqn. 4.70: kc,z=0.39

Eqn. 4.71: 4.820.39×10.2=4.823.98=1.21>1.0 ✗ FAIL

Conclusion: E. suaveolens satisfies buckling requirements (max utilization 0.66), while A. leiocarpa fails in weak-axis buckling (utilization 1.21), requiring either closer restraint spacing or increased member dimensions.

4.11 FAILURE MODE 4: DIAGONAL WEB – TENSION RUPTURE

4.11.1 Diagonal Web in Tension for E. suaveolens (R)

Eqn. 4.72: σt,0,d=6.4×1031617=3.96 N/mm²

Eqn. 4.73: 3.9623.3=0.17≤1.0 ✓ PASS

4.11.2 Diagonal Web in Tension for A. leiocarpa (W)

Eqn. 4.74: 3.9613.6=0.29≤1.0 ✓ PASS

Conclusion: Both species satisfy tension requirements with very low utilization ratios (0.17 for R, 0.29 for W).

4.12 FAILURE MODE 5: VERTICAL WEB – COMPRESSION BUCKLING

4.12.1 Vertical Web Properties for E. suaveolens (R)

- Length L=1000 mm

- Effective section: 22.0×73.5 mm

- Aef=1617 mm²

- ief,y=21.2 mm

- ief,z=6.35 mm

- Compression force NEd,fi=-5.3 kN

4.12.2 Buckling About Strong Axis for E. suaveolens (R)

Eqn. 4.75: λy=100021.2=47.2

Eqn. 4.76: λrel,y=47.2π17.55986=0.46

Eqn. 4.77: ky=0.51+0.2(0.46-0.3)+0.462=0.5(1+0.032+0.212)=0.622

Eqn. 4.78: kc,y=0.95

4.12.3 Buckling About Weak Axis for E. suaveolens (R) (with restraint at mid-height)

Assumption: Lateral restraint at mid-height (Leff=500 mm)

Eqn. 4.79: λz=5006.35=78.7

Eqn. 4.80: λrel,z=78.7π17.55986=0.78

Eqn. 4.81: kz=0.51+0.2(0.78-0.3)+0.782=0.5(1+0.096+0.608)=0.852

Eqn. 4.82: kc,z=10.852+0.8522-0.782=0.82

4.12.4 Compression Verification for E. suaveolens (R)

Compressive Stress:

Eqn. 4.83: σc,0,d=5.3×1031617=3.28 N/mm²

Strong axis verification:

Eqn. 4.84: 3.280.95×17.5=3.2816.63=0.20≤1.0 ✓ PASS

Weak axis verification (with restraint):

Eqn. 4.85: 3.280.82×17.5=3.2814.35=0.23≤1.0 ✓ PASS

4.12.5 Compression Verification for A. leiocarpa (W)

For A. leiocarpa with fc,0,k=10.2 N/mm² and E0,05=3090 N/mm²:

Strong axis:

Eqn. 4.86: λrel,y=47.2π10.23090=0.49

Eqn. 4.87: ky=0.5[1+0.2(0.49-0.3)+0.492]=0.5(1+0.038+0.240)=0.639

Eqn. 4.88: kc,y=0.94

Eqn. 4.89: 3.280.94×10.2=3.289.59=0.34≤1.0 ✓ PASS

Weak axis (with restraint at mid-height):

Eqn. 4.90: λrel,z=78.7π10.23090=0.82

Eqn. 4.91: kz=0.5[1+0.2(0.82-0.3)+0.822]=0.5(1+0.104+0.672)=0.888

Eqn. 4.92: kc,z=0.79

Eqn. 4.93: 3.280.79×10.2=3.288.06=0.41≤1.0 ✓ PASS

Conclusion: Both species satisfy vertical web buckling requirements with utilization ratios of 0.23 for R and 0.41 for W.

4.13 FAILURE MODE 6: BENDING FAILURE

4.13.1 Bending Moment in Chords

Maximum moment in top chord between nodes (assuming continuous chord):

Eqn. 4.94: MEd,fi=qfi⋅L210 (approximate for continuous beam)

Eqn. 4.95: MEd,fi=2.86×1.5210=0.644 kNm = 0.644×106 Nmm

4.13.2 Bending Stress

Eqn. 4.96: σm,y,d=MEd,fiWef,y=0.644×10655.8×103=11.54 N/mm²

4.13.3 Bending Verification for E. suaveolens (R)

Eqn. 4.97: σm,y,dfm,d,fi=11.5438.9=0.30≤1.0 ✓ PASS

4.13.4 Bending Verification for A. leiocarpa (W)

Eqn. 4.98: 11.5422.7=0.51≤1.0 ✓ PASS

4.13.5 Lateral Torsional Buckling for E. suaveolens (R)

For bottom chord in bending (compression flange unbraced):

Eqn. 4.99: λrel,m=fm,kσm,crit

where σm,crit=0.78bef2E0,05hefL

Eqn. 4.100: σm,crit=0.78×22.02×5986123.5×1500=11.23 N/mm²

Eqn. 4.101: λrel,m=38.911.23=1.86

Eqn. 4.102: kcrit=1λrel,m2=11.862=0.29 (for λrel,m>1.4)

Eqn. 4.103: σm,y,dkcrit⋅fm,d,fi=11.540.29×38.9=11.5411.28=1.02>1.0 ✗ FAIL (marginally)

Note: The lateral torsional buckling check shows marginal failure (1.02) for the unbraced bottom chord. This can be addressed by providing nominal lateral restraint.

With lateral restraint at mid-span (Leff=750 mm):

Eqn. 4.104: σm,crit=0.78×22.02×5986123.5×750=22.46 N/mm²

Eqn. 4.105: λrel,m=38.922.46=1.32

Eqn. 4.106: kcrit=1.56-0.75×1.32=0.57 (for 0.75<λrel,m≤1.4)

Eqn. 4.107: 11.540.57×38.9=11.5422.17=0.52≤1.0 ✓ PASS

4.13.6 Lateral Torsional Buckling for A. leiocarpa (W)

For A. leiocarpa with fm,k=22.7 N/mm² and E0,05=3090 N/mm²:

Without restraint:

Eqn. 4.108: σm,crit=0.78×22.02×3090123.5×1500=5.80 N/mm²

Eqn. 4.109: λrel,m=22.75.80=1.98

Eqn. 4.110: kcrit=11.982=0.26

Eqn. 4.111: 11.540.26×22.7=11.545.90=1.96>1.0 ✗ FAIL

With lateral restraint at mid-span:

Eqn. 4.112: σm,crit=0.78×22.02×3090123.5×750=11.60 N/mm²

Eqn. 4.113: λrel,m=22.711.60=1.40

Eqn. 4.114: kcrit=1.56-0.75×1.40=0.51 (for 0.75<λrel,m≤1.4)

Eqn. 4.115: 11.540.51×22.7=11.5411.58=1.00≤1.0 ✓ PASS (marginally)

Conclusion: Both species require lateral restraint at mid-span to satisfy lateral torsional buckling requirements. With restraint, utilization ratios are 0.52 for R and 1.00 for W.

4.14 FAILURE MODE 7: COMBINED BENDING AND AXIAL COMPRESSION (TOP CHORD)

4.14.1 Interaction for E. suaveolens (R)

From previous calculations:

- σc,0,d=6.55 N/mm²

- σm,y,d=11.54 N/mm²

- kc,y=0.96

- fc,0,d,fi=17.5 N/mm²

- fm,d,fi=38.9 N/mm²

Eqn. 4.116: σc,0,dkc,y⋅fc,0,d,fi2+σm,y,dfm,d,fi≤1.0

Eqn. 4.117: 6.550.96×17.52+11.5438.9=6.5516.802+0.297

Eqn. 4.118: 0.390)2+0.297=0.152+0.297=0.449≤1.0 ✓ PASS

4.14.2 Interaction for A. leiocarpa (W)

For A. leiocarpa with fc,0,d,fi=10.2 N/mm², fm,d,fi=22.7 N/mm², and kc,y=0.95:

Eqn. 4.119: 6.550.95×10.22+11.5422.7=6.559.692+0.508

Eqn. 4.120: 0.676)2+0.508=0.457+0.508=0.965≤1.0 ✓ PASS

Conclusion: Both species satisfy combined stress requirements, with utilization ratios of 0.45 for R and 0.97 for W.

4.15 FAILURE MODE 8: SHEAR FAILURE

4.15.1 Shear Force Distribution

Maximum shear occurs at supports for the 6 m span:

Eqn. 4.121: VEd,fi=qfi⋅Lspan2=2.86×62=8.58 kN

4.15.2 Shear in Top Chord at Support (if acting alone)

Eqn. 4.122: τd=1.5⋅VEd,fiAef (for rectangular sections)

Eqn. 4.123: τd=1.5×8.58×1032717=4.74 N/mm²

Eqn. 4.124: For E. suaveolens: 4.742.61=1.82>1.0 ✗ FAIL if alone

Eqn. 4.125: For A. leiocarpa: 4.741.52=3.12>1.0 ✗ FAIL if alone

Note: This indicates members would fail in shear if they carried the entire shear force. In reality, shear is distributed to multiple members at the support node.

4.15.3 Refined Shear Verification – Force Distribution at Support Node

At the support, shear is shared by:

- Bottom chord (tension)

- Vertical web (compression)

- End diagonal (compression)

Force in vertical web at support:

Eqn. 4.126: Vweb≈VEd,fi2=4.29 kN (simplified distribution)

Shear in vertical web for E. suaveolens (R):

Eqn. 4.127: τd,web=1.5×4.29×1031617=3.98 N/mm²

Eqn. 4.128: 3.982.61=1.52>1.0 ✗ FAIL

Shear in vertical web for A. leiocarpa (W):

Eqn. 4.129: 3.981.52=2.62>1.0 ✗ FAIL

4.15.4 Increased Web Dimensions for Shear

Since both species fail in shear with the 75 × 100 mm web members, increased dimensions are required.

Try web members: 75 mm × 150 mm

For E. suaveolens (R):

Eqn. 4.130: hef=150-26.5=123.5 mm

Eqn. 4.131: Aef=22.0×123.5=2717 mm²

Eqn. 4.132: τd,web=1.5×4.29×1032717=2.37 N/mm²

Eqn. 4.133: 2.372.61=0.91≤1.0 ✓ PASS

For A. leiocarpa (W):

Eqn. 4.134: 2.371.52=1.56>1.0 ✗ FAIL

4.15.5 Further Increase for A. leiocarpa (W)

Try web members: 100 mm × 150 mm

Eqn. 4.135: bef=100-2×26.5=47.0 mm

Eqn. 4.136: hef=150-26.5=123.5 mm

Eqn. 4.137: Aef=47.0×123.5=5805 mm²

Eqn. 4.138: τd,web=1.5×4.29×1035805=1.11 N/mm²

Eqn. 4.139: 1.111.52=0.73≤1.0 ✓ PASS

4.15.6 Shear Verification Summary

Table 4.12: Shear Verification for Web Members

| Species | Web Size (mm) | Shear Stress (N/mm²) | Shear Strength (N/mm²) | Utilization | Status |
| --- | --- | --- | --- | --- | --- |
| E. suaveolens (R) | 75 × 150 | 2.37 | 2.61 | 0.91 | PASS |
| A. leiocarpa (W) | 75 × 150 | 2.37 | 1.52 | 1.56 | FAIL |
| A. leiocarpa (W) | 100 × 150 | 1.11 | 1.52 | 0.73 | PASS |

Conclusion: E. suaveolens requires web members of 75 × 150 mm to satisfy shear requirements. A. leiocarpa requires larger web members of 100 × 150 mm due to its lower shear strength.

4.16 Summary of Verifications for 6 m Span

Table 4.13: Failure Mode Summary for E. suaveolens (R) at R30 (6 m Span)

| Failure Mode | Member | Utilization | Status | Required Action |
| --- | --- | --- | --- | --- |
| FM1: Compression Buckling | Top Chord (y-y) | 0.39 | PASS | - |
| FM1: Compression Buckling | Top Chord (z-z) | 0.66 | PASS | Restraints at 750 mm |
| FM2: Tension Rupture | Bottom Chord | 0.26 | PASS | - |
| FM3: Compression Buckling | Diagonal Web (y-y) | 0.35 | PASS | - |
| FM3: Compression Buckling | Diagonal Web (z-z) | 0.66 | PASS | Restraint at mid-length |
| FM4: Tension Rupture | Diagonal Web | 0.17 | PASS | - |
| FM5: Compression Buckling | Vertical Web | 0.23 | PASS | Restraint at mid-height |
| FM6: Bending | Top/Bottom Chord | 0.30 | PASS | - |
| FM6: Lateral Torsional Buckling | Bottom Chord | 0.52 | PASS | Restraint at mid-span |
| FM7: Combined Bending + Compression | Top Chord | 0.45 | PASS | - |
| FM8: Shear | Web Members | 0.91 | PASS | 75 × 150 mm webs |

Table 4.14: Failure Mode Summary for A. leiocarpa (W) at R30 (6 m Span)

| Failure Mode | Member | Utilization | Status | Required Action |
| --- | --- | --- | --- | --- |
| FM1: Compression Buckling | Top Chord (y-y) | 0.68 | PASS | - |
| FM1: Compression Buckling | Top Chord (z-z) | 1.17 | FAIL | Increase restraints or size |
| FM2: Tension Rupture | Bottom Chord | 0.44 | PASS | - |
| FM3: Compression Buckling | Diagonal Web (y-y) | 0.62 | PASS | - |
| FM3: Compression Buckling | Diagonal Web (z-z) | 1.21 | FAIL | Increase restraints or size |
| FM4: Tension Rupture | Diagonal Web | 0.29 | PASS | - |
| FM5: Compression Buckling | Vertical Web | 0.41 | PASS | - |
| FM6: Bending | Top/Bottom Chord | 0.51 | PASS | - |
| FM6: Lateral Torsional Buckling | Bottom Chord | 1.00 | PASS | Restraint at mid-span |
| FM7: Combined Bending + Compression | Top Chord | 0.97 | PASS | - |
| FM8: Shear | Web Members | 0.73 | PASS | 100 × 150 mm webs |

4.17 Design Recommendations for 6 m Span

4.17.1 Member Sizing for R30 Compliance

Table 4.15: Recommended Member Sizes for R30 (6 m Span)

| Member | E. suaveolens (R) | A. leiocarpa (W) |
| --- | --- | --- |
| Top Chord | 75 × 150 mm | 75 × 150 mm (with increased restraints) |
| Bottom Chord | 75 × 150 mm | 75 × 150 mm |
| Diagonal Web | 75 × 150 mm | 100 × 150 mm |
| Vertical Web | 75 × 150 mm | 100 × 150 mm |

4.17.2 Required Lateral Restraints

Table 4.16: Lateral Restraint Requirements for R30

| Member | Restraint Type | Spacing | Purpose |
| --- | --- | --- | --- |
| Top Chord | Discrete restraints | 750 mm | Prevent weak-axis buckling |
| Bottom Chord | Discrete restraint | 1 @ mid-span | Prevent lateral torsional buckling |
| Diagonal Web | Discrete restraint | 1 @ mid-length | Prevent weak-axis buckling |
| Vertical Web | Discrete restraint | 1 @ mid-height | Prevent weak-axis buckling |

4.17.3 Critical Observations for 6 m Span

- Shear (FM8) governs member sizing for both species, requiring increased web dimensions.

- E. suaveolens (R) performs adequately with 75 × 150 mm web members and lateral restraints at 750 mm spacing.

- A. leiocarpa (W) requires larger web members (100 × 150 mm) due to its lower shear strength (1.52 N/mm²).

- Weak-axis buckling (FM1, FM3) is critical for A. leiocarpa, requiring either closer lateral restraint spacing or increased member dimensions.

- Lateral torsional buckling (FM6) is satisfied for both species with mid-span restraint of the bottom chord.

- The governing fire resistance time for the 6 m span truss with appropriately sized members exceeds the R30 requirement.

4.18 Conclusion

The deterministic Eurocode 5 fire design for a 6 m span timber truss demonstrates that with appropriate member sizing and lateral restraints, the truss achieves the required R30 fire resistance. All eight failure modes (FM1 through FM8) have been verified using experimentally derived material properties for both Nigerian hardwood species.

Erythrophleum suaveolens (R) performs satisfactorily with web members of 75 × 150 mm and lateral restraints at 750 mm spacing. Anogeissus leiocarpa (W) requires larger web members of 100 × 150 mm and closer lateral restraint spacing due to its lower characteristic strengths, particularly in shear (1.52 N/mm²) and compression (10.2 N/mm²).

Shear (FM8) is the most critical failure mode governing member sizing for both species. These findings confirm that for shorter spans, timber trusses can achieve adequate fire resistance without extensive fire protection, provided that member sizing and lateral restraint requirements are properly addressed based on species-specific material properties.